Harald Morgner

Reconstruction of concentration depth profiles by means of ARXPS

The model:

The surface region is conceived to be consist of several layers j=1..jmax. Beyond the last layer the composition is that of the bulk. The layers are characterized by number densities ni(j) where the suffix i refers to the species i. The composition within a layer is homogeneous.

dj

j=1

=2

=3

j=jmax



bulk

Numbering of layers: j

Numbering of components: i

Number density of component i in layer j is given as ni(j)

Thickness of layer j:   dj

Observation depth λ'=λcosθ is product of mean free path λand cosθ

------------------------------------------------------------------------------------------------------------

Contribution from homogeneous material without overlayer

Ii, bulk, λ'=qinibulkλ'

------------------------------------------------------------------------------------------------------------

Contribution from homogeneous material with overlayers

j=1

j=jmax

Ii, bulk, λ'=qinibulkλ'⋅jmaxj=1exp−djλ'

---------------------------------------------------------------------------------------------------------------

# Contribution from species i in layer j

Ii, j, θ=qi ⋅ nij ⋅ λ' ⋅ 1−exp−djλ'j−1j=1exp−djλj''

Photoionization cross section for species i

observation depth

number density of species i in layer j

wobei die

Variation of the number densities ni(j) until the calculated intensities agree with the experimental intensities within the experimental errors.

iIexpi, λ'−Icalci, λ'ΔIexpi, λ'2=deviation

Standard-method for this fitting process is Marquardt-fit

Disadvantage:	may end in a local minimum

Genetic Algorithm is very robust and yields estimate of accuracy

Recommended reference: Eschen et al, J. Phys. Condens. Matter 7  (1995) 1961-78

-----------------------------------------------------------------------------------------------------------------

Remark:

The direct determination of the concentration depth profiles via Inverse Laplace Transformation is only a theoretical possibility

The Laplace Transformed Fs of the function ft is given by the expression

Lft=Fs=0∞exp−st⋅ftdt

In principal the inversion can be carried out, i.e. ft can be reconstructed from Fs

The task to be carried out for constructing the concentration depth profiles has the same mathematical structure as constructing the inverse Laplace transformed.

The expression

Iiλ'=0∞niz e−z⋅1λ' dz

can be conceived as Laplace Transformed of  niz. Thus, the construction of niz from Iiλ' could be done. In practice, this attempt fails because already small uncertainties in Iiλ' render the result for niz unreliable.